## Slide 1
Dynamical Mean Field Theory on FeO under pressure
Ronald Cohen
Geophysical Laboratory
Carnegie Institution of Washington
cohen@gl.ciw.edu
2012 Summer School on Computational Materials Science Quantum Monte Carlo: Theory and Fundamentals
July 23–-27, 2012 • University of Illinois at Urbana–Champaign
http://www.mcc.uiuc.edu/summerschool/2012/
QMC Summer School 2012 UIUC

## Slide 3: Background: FeO
At ambient pressure FeO is an antiferromagnetic insulator with a rock salt structure
Iron 3d states partially filled, but localized
Borderline between charge transfer and Mott insulator
Difficult to make stoichiometric FeO in the lab at low pressures (vacancies yield Fe1-xO where x ~ 0.07) but stoichiometric under pressure
The phase diagram as of
1994 (Fei and Mao, Science,
266, 1678, 1994)
Knittle and Jeanloz, JGR 1991

## Slide 4: FeO wüstite is an insulator at ambient conditions
LDA/GGA etc. make it a metal
Cohen et al. (1998) High-Pressure Materials Research. Materials Research Society. 499.
LDA+U does open a gap in AFM rhombohedral or lower symmetry FeO and predicts a metal insulator transition under pressure, but not a high-spin low-spin transition. (Gramsch, Cohen, and Savrasov, Am. Mineral., 88, 257 (2003).
LDA+U is a model, and how accurate it is unknown.
LDA+U cannot give a gap in paramagnetic FeO.

## Slide 5
Extended Stoner model
Increase in bandwidth causes spin collapse:

## Slide 6: Magnetic collapse vs. High-spin low-spin transition vs. Orbital ordering in FeO
Moment 4μB
4 t2g 2 eg
Moment 0
6 t2g
t2g
t2g
t2g
eg
eg

## Slide 8: LDA-DMFT
Lattice Problem (DFT) LAPW
Atomic Problem
(Many-body theory: DMFT)
Lattice Problem (contains geometry)
Impurity Model (CTQMC)
HDFT
Gimp
New density
Fully self-consistent, finite temperature

## Slide 9: DFT-DMFT
Crystal problem
“Impurity” problem
Self-consistency condition
Kristjan Haule DFT-DMFT code:
integrates wien2k LAPW code for Crystal with Continuous Time Quantum Monte Carlo (CTQMC) for impurity
Fully self-consistent in charge density ρ, chemical potential μ, impurity levels Eimp, hybridization Δ, and self-energy Σ.
Calculations are done on imaginary frequency ω axis, and analytically continued to real axis.
No down folding, fully self-consistent

## Slide 10
Haule

## Slide 11: Continuous Time Quantum Monte Carlo (CTQMC) QMC over Feynman diagrams Imaginary time (frequency)
Haule

## Slide 12: CTQMC
β
0

## Slide 13: Imaginary Time Gf V=540au
it
it
G
G
300K
2000K
DOS at Ef=0
DOS at Ef≠0
t2g
t2g
eg
eg
occupancy
0
6
40
0

## Slide 14: Histogram of number of kinks on Feynman diagrams
300K
2000K
Number of kinks
1000
0
500
V/V0=1, High Spin

## Slide 15: Experimental evidence of metallization at high P and T
Ohta, Cohen, et al., PRL 2012
Kenji Ohta, Katsuya Shimizu, Osaka University, Yasuo Ohishi, Japan Synchrotron Radiation Research Institute, Kei Hirose, Tokyo Institute of Technology

## Slide 16: FeO Density of States
Ohta et al., 2011

## Slide 17: DC conductivity versus pressure

## Slide 18: DMFT orbital occupancy transition (HS-LS crossover)
Using experimental equation of state:
from Fischer et al. EPSL 2011

## Slide 19: Spectral Function A(k,ω)
V=405 au, V/V0=0.75, 68 GPa 300K
V=405 au, V/V0=0.75, 88 GPa 2000K
Low spin insulator -> low spin metal

## Slide 20: High spin at low P
V=540 au, V/V0=1
eg2 t2g4
HS
d5
d7

## Slide 21: Spin fluctuations  metallization
V=405 au, V/V0=0.75, 68 GPa 300K
V=405 au, V/V0=0.75, 88 GPa 2000K
eg0 t2g6
eg2 t2g4
LS
HS

## Slide 22: FeO phase diagram 1/12
Ohta, Cohen, et al., PRL, 2012

## Slide 23
A new kind of metal in the deep Earth - Worldnews.com
article.wn.com/view/ A_new_kind_of_metal_in_the_deep_Earth/
Dec 19, 2011 – Read full article. Back to 'A new kind of metal in the deep Earth' .... 10 years ago, Ronald Cohen had made a name for himself in private equity.

## Slide 24: Summary
DFT-DMFT computations show metallization in FeO at high P and T
  Temperature is crucial.
  Metallization is due to fluctuations between high-and low-spin states.
  Self-consistency is crucial.
  Excellent agreement with experiment.